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PIASTRA DI BASE
Piastra di base, dimensionata considerando il massimo momento resistente alla base del palo considerato, saldata al palo da saldatori qualificati dall I.I.S. Istituto Italiano della Saldatura e controllo qualità saldature secondo EN ISO 3834.
I tirafondi sono in tondino di acciaio, grezzi e completi di bulloneria zincata. 
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	Codice prodotto
	Descrizione
	peso kg
	Codice prodotto
	Descrizione

	+P (MAXD131)
	palo max D131 ... con piastra base quadrata 250x15 saldata, 4 fori asolati d20 interasse 170x170
	
	TRFM16X750U3D2R
	Tirafondo acciaio S355J2, M16 L.Sv.750, curvato a uncino R.48 unghia 75 con 1 estremità filettata L.100, grezzo + 3 dadi medi M16 e 2 rondelle piane (17x48x4) zinc.el., tutto montato

	+P (MAXD172)
	palo max D172 ... con piastra base quadrata 300x15 saldata, 4 fori asolati d22 interasse 220x220
	
	TRFM18X750U3D2R
	Tirafondo acciaio S355J2, M18 L.Sv.750, curvato a uncino R.54 unghia 75 con 1 estremità filettata L.100, grezzo + 3 dadi medi M18 e 2 rondelle piane (20x54x4) zinc.el., tutto montato

	+P (MAXD219)
	palo max D219 ... con piastra base quadrata 350x20 saldata, 4 fori asolati d24 interasse 270x270
	
	TRFM20X1000U3D2R
	Tirafondo acciaio S355J2, M20 L.Sv.1000, curvato a uncino R.60 unghia 100 con 1 estremità filettata L.120, grezzo + 3 dadi medi M20 e 2 rondelle piane (22x60x4) zinc.el., tutto montato

	+P (MAXD250)
	palo max D250 ... con piastra base quadrata 400x20 saldata, 4 fori asolati d24 interasse 300x300
	
	TRFM20X1000U3D2R
	Tirafondo acciaio S355J2, M20 L.Sv.1000, curvato a uncino R.60 unghia 100 con 1 estremità filettata L.120, grezzo + 3 dadi medi M20 e 2 rondelle piane (22x60x4) zinc.el., tutto montato

	+P (MAXD320)
	palo max D320 ... con piastra base quadrata 475x20 saldata, 4 fori asolati d28 interasse 380x380
	
	TRFM24X1200U3D2R
	Tirafondo acciaio S355J2, M24 L.Sv.1200, curvato a uncino R.72 unghia 120 con 1 estremità filettata L.140, grezzo + 3 dadi medi M24 e 2 rondelle piane (26x72x5) zinc.el., tutto montato

	+P (MAXD370)
	palo max D370 ... con piastra base quadrata 525x25 saldata, 4 fori asolati d28 interasse 430x430
	
	TRFM24X1200U3D2R
	Tirafondo acciaio S355J2, M24 L.Sv.1200, curvato a uncino R.72 unghia 120 con 1 estremità filettata L.140, grezzo + 3 dadi medi M24 e 2 rondelle piane (26x72x5) zinc.el., tutto montato

	+P (MAXD450)
	palo max D450 ... con piastra base quadrata 625x25 saldata, 4 fori asolati d31 interasse 520x520
	
	TRFM27X1500U3D2R
	Tirafondo acciaio S355J2, M27 L.Sv.1500, curvato a uncino R.81 unghia 150 con 1 estremità filettata L.160, grezzo + 3 dadi medi M27 e 2 rondelle piane (30x81x6) zinc.el., tutto montato


BASE PLATE

Base plate designed considering the maximum moment of resistance at the base of the considered column, welded to the column by welders qualified by the I.I.S. (Italian Institute of Welding) and with welding quality check according to EN ISO 3834.

The anchor bolts are made of steel rod, blank and completed with galvanised bolts and washers. 


	Product Code
	Description
	weight kg
	Product Code
	Description

	+P (MAXD131)
	column max D131 ... with welded square base plate 250x15, 4 slotted holes d20 spacing 170x170
	
	TRFM16X750U3D2R
	Anchor bolt steel grade S355J2, M16 L.Dev.750, curved "J" type R.48 hook 75 with 1 threaded end L.100, blank + 3 medium nuts M16 and 2 plain washers (17x48x4) electrogalvanised, all mounted

	+P (MAXD172)
	column max D172 ... with welded square base plate 300x15, 4 slotted holes d22 spacing 220x220
	
	TRFM18X750U3D2R
	Anchor bolt steel grade S355J2, M18 L.Dev.750, curved "J" type R.54 hook 75 with 1 threaded end L.100, blank + 3 medium nuts M18 and 2 plain washers (20x54x4) electrogalvanised, all mounted 

	+P (MAXD219)
	column max D219 ... with welded square base plate 350x20, 4 slotted holes d24 spacing 270x270
	
	TRFM20X1000U3D2R
	Anchor bolt steel grade S355J2, M20 L.Dev.1000, curved "J" type R.60 hook 100 with 1 threaded end L.120, blank + 3 medium nuts M20 and 2 plain washers (22x60x4) electrogalvanised, all mounted 

	+P (MAXD250)
	column max D250 ... with welded square base plate 400x20, 4 slotted holes d24 spacing 300x300
	
	TRFM20X1000U3D2R
	Anchor bolt steel grade S355J2, M20 L.Dev.1000, curved "J" type R.60 hook 100 with 1 threaded end L.120, blank + 3 medium nuts M20 and 2 plain washers (22x60x4) electrogalvanised, all mounted 

	+P (MAXD320)
	column max D320 ... with welded square base plate 475x20, 4 slotted holes d28 spacing 380x380
	
	TRFM24X1200U3D2R
	Anchor bolt steel grade S355J2, M24 L.Dev.1200, curved "J" type R.72 hook 120 with 1 threaded end L.140, blank + 3 medium nuts M24 and 2 plain washers (26x72x4) electrogalvanised, all mounted 

	+P (MAXD370)
	column max D370 ... with welded square base plate 525x25, 4 slotted holes d28 spacing 430x430
	
	TRFM24X1200U3D2R
	Anchor bolt steel grade S355J2, M24 L.Dev.1200, curved "J" type R.72 hook 120 with 1 threaded end L.140, blank + 3 medium nuts M24 and 2 plain washers (26x72x4) electrogalvanised, all mounted 

	+P (MAXD450)
	column max D450 ... with welded square base plate 625x25, 4 slotted holes d31 spacing 520x520
	
	TRFM27X1500U3D2R
	Anchor bolt steel grade S355J2, M27 L.Dev.1500, curved "J" type R.81 hook 150 with 1 threaded end L.160, blank + 3 medium nuts M27 and 2 plain washers (30x81x6) electrogalvanised, all mounted 
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