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PALI SEMAFORICI O PEDONALI OTTAGONALI RICURVI, TIPO COSEM........

Pali semaforici a sezione ottagonale con sbraccio curvato, realizzata da azienda certificata ISO9001 e in possesso di autorizzazione quale centro di trasformazione secondo DM 14/01/08, marca palicampion, tipo COSEM…., composti da 2 elementi (piedritto+sbraccio) da assemblare in opera mediante incastro forzato per sovrapposizione, ottenuti mediante formatura a freddo di lamiera in acciaio S355JO EN 10025 e successiva saldatura longitudinale esterna eseguita con procedimento automatico omologato dall I.I.S. (Istituto Italiano della Saldatura) e controllo qualità saldature secondo EN ISO 3834.

I pali, predisposti per l’ancoraggio al basamento mediante infissione nel blocco di fondazione, sono completi delle 3 lavorazioni standard alla base per il collegamento elettrico a norma, asola entrata cavi, attacco m.a.t., asola per morsettiera. Sbraccio curvato con raggio 1800.

Tolleranze dimensionali UNI EN 40/2 - UNI EN 10051.

Protezione contro la corrosione mediante zincatura a caldo, ottenuta con il seguente ciclo: grassaggio; decapaggio; lavaggio; flussaggio; preriscaldo; zincatura in zinco fuso a 440÷450 gradi centigradi, con percentuale minima di zinco nel bagno di zincatura ( 98.5%. Rivestimento ottenuto conforme alla norma UNI EN ISO 1461 con spessori minimi di 55 microns e medi di 70 microns.

Pali dimensionati secondo la normativa vigente considerando i carichi del vento previsti dal D.M. 16/01/96, con 1 o 2 pannelli di contrasto 90x135 cm, applicati sullo sbraccio.
	Codice prodotto
	Descrizione

	COSEM43
	Palo ottagonale curvato in acciaio laminato a caldo ad alta resistenza EN10025, 7500x4000x170x76, piedritto+braccio ad incastro, infissione 1000 entrata cavi, m.a.t., asola 186x46, zincato ISO1461. Marcatura CE-EN1090

	COSEM48
	Palo ottagonale curvato in acciaio laminato a caldo ad alta resistenza EN10025, 7500x4000x170x76, piedritto+braccio ad incastro, infissione 1000, entrata cavi, m.a.t., asola 186x46, zincato  ISO1461. Marcatura CE-EN1090

	COSEM53
	Palo ottagonale curvato in acciaio laminato a caldo ad alta resistenza EN10025, 7500x5000x195x91, piedritto+braccio ad incastro, infissione 1000, entrata cavi, m.a.t., asola 186x46, zincato ISO1461. Marcatura CE-EN1090

	COSEM58
	Palo ottagonale curvato in acciaio laminato a caldo ad alta resistenza EN10025, 7500x5000x240x90, piedritto+braccio ad incastro, infissione 1000, entrata cavi, m.a.t., asola 186x46, zincato ISO1461. Marcatura CE-EN1090

	COSEM63
	Palo ottagonale curvato in acciaio laminato a caldo ad alta resistenza EN10025, 7500x6000x210x97, piedritto+braccio ad incastro, infissione 1000, entrata cavi, m.a.t., asola 186x46, zincato ISO1461. Marcatura CE-EN1090

	COSEM68
	Palo ottagonale curvato in acciaio laminato a caldo ad alta resistenza EN10025, 7500x6000x240x90, piedritto+braccio ad incastro, infissione 1000, entrata cavi, m.a.t., asola 186x46, zincato ISO1461. Marcatura CE-EN1090


TRAFFIC LIGHT COLUMNS OR OCTAGONAL CURVED PEDESTRIAN COLUMNS, TYPE COSEM........

Octagonal traffic light columns with curved bracket, made by a company ISO9001 certified and having authorisation as processing centre according to DM 14/01/08, brand palicampion, COSEM…., composed of 2 elements (shaft+bracket) to be assembled at site by forced overlapping, obtained by cold bending of steel plate grade S235JR EN 10025 and subsequent external longitudinal welding carried out with automatic process approved by the I.I.S. (Italian Institute of Welding) and with welding quality check according to EN ISO 3834.
The columns, provided for the anchorage to the basement by direct planting into the foundation block, are completed with 3 standard works at the base for the electric wiring according to the standard: cable entry slot, earthing connection, slot for junction box housing. Curved bracket with radius 1800.

Tolerances on dimensions UNI EN 40/2 - UNI EN 10051.

Protection against corrosion by means of hot dip galvanization obtained with the following cycle: degreasing; pickling, washing, fluxing, pre heating; hot dip galvanization in melted zinc bath at 440÷450°, with minimum percentage of zinc into the bath ( 98.5%. Coating obtained according to UNI EN ISO 1461 with minimum thickness 55 microns et average 70 microns.

Columns designed according to the standard in force considering the wind load requested by  D.M. 16/01/96, with 1 or 2 panels 90x135 cm, installed on the bracket.

	Product code
	Description

	COSEM43
	Curved octagonal column in hot-rolled high-strength steel EN10025, 7500x4000x170x76, overlapped shaft+bracket, planting depth 1000, cable entry, earth connection, slot 186x46, galvanised ISO1461. Marking CE-EN1090

	COSEM48
	Curved octagonal column in hot-rolled high-strength steel EN10025, 7500x4000x170x76, overlapped shaft+bracket, planting depth 1000, cable entry, earth connection, slot 186x46, galvanised ISO1461. Marking CE-EN1090

	COSEM53
	Curved octagonal column in hot-rolled high-strength steel EN10025, 7500x5000x195x91, overlapped shaft+bracket, planting depth 1000, cable entry, earth connection, slot 186x46, galvanised ISO1461. Marking CE-EN1090

	COSEM58
	Curved octagonal column in hot-rolled high-strength steel EN10025, 7500x5000x240x90, overlapped shaft+bracket, planting depth 1000, cable entry, earth connection, slot 186x46, galvanised ISO1461. Marking CE-EN1090

	COSEM63
	Curved octagonal column in hot-rolled high-strength steel EN10025, 7500x6000x210x97, overlapped shaft+bracket, planting depth 1000, cable entry, earth connection, slot 186x46, galvanised ISO1461. Marking CE-EN1090

	COSEM68
	Curved octagonal column in hot-rolled high-strength steel EN10025, 7500x6000x240x90, overlapped shaft+bracket, planting depth 1000, cable entry, earth connection, slot 186x46, galvanised ISO1461. Marking CE-EN1090
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