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PALI PER ILLUMINAZIONE E ARREDO URBANO MODELLO “ACROPOLIS”

Voce di capitolato

Palo speciale per illuminazione e arredo urbano collezione “iPaliarredo” serie “Old” modello “ACROPOLIS”, altezza ~ 3,2 metri fuori terra, interamente realizzato in fusione di ghisa grosso spessore, costituito da 2 elementi sovrapponibili con viti di bloccaggio a scomparsa.

( Basamento altezza 800, di forma troncoconica, con scanalature e rilievi, d.base 230, piastra di appoggio 280x280 da fissare con 4 tirafondi ancorati alla fondazione, portello di accesso alla morsettiera interna

( Colonna superiore troncoconica lunghezza, 2450, base decorata con foglie, scanalature longitudinali, capitello superiore, estremità predisposta per attacco corpo illuminante o sbraccio
( Morsettiera 235x70x45, classe II doppio isolamento, CEI EN 60668-1, CEI EN 60998-2-1, contenitore IP54, 4 poli a 3 vie, dorsale in/out 4x2.5-16 mmq, derivazione 4x1,5-4 mmq, 1 portafus. sezionabile 8,5x31,5 max 10A su guida DIN. 

Protezione contro la corrosione delle parti in ghisa mediante metallizzazione. 
Verniciatura estetica esterna, colore (a scelta dalla cartella colori: nero, antracite, marrone, ombra, granito, grafite, verde, reseda, acciaio, oltremare, polvere, alluminio, rubino, castagna, avorio, bianco) ad effetto raggrinzato, ottenuto con ciclo a polveri termoindurenti, comprensivo di: pulizia da eventuali residui di zincatura; lisciatura delle superfici mediante leggera azione meccanica; pulizia delle superfici al fine di eliminare olio e sporco in genere e creare una buona base di aderenza; applicazione mediate spruzzatura elettrostatica della polvere poliestere adatta per superfici zincate a caldo destinate all’esterno, fino a raggiungere 60/80 micron di spessore; polimerizzazione in forno a temperatura costante di circa 200° per 40-50 minuti, imballo per ogni singolo palo, mediante fasciatura con tessuto non tessuto “cisellina” agugliato e calandrato a caldo 100% poliestere, (non si accetta fasciatura in pluriboll), per evitare danneggiamenti della verniciatura durante le operazioni di movimentazione, trasporto e stoccaggio. Le caratteristiche del rivestimento ottenuto saranno: spessore medio 60 micron, resistenza ai test di quadrettatura ISO2409, resistenza ai test d’urto UNI8901

LIGHTING AND DECORATIVE COLUMNS MODEL  “ACROPOLIS”

Tender Specification
Special lighting and decorative column “iPaliarredo” collection “Old” series model “ACROPOLIS”, height ~ 3,2 meters above ground, completely made in die cast iron big thickness, composed of two superimposed elements with not visible fixing screws.

( Basement height 800, conical shape, with grooves relieves, d.base 230, bearing plate 280x280 to be fixed with 4 anchor bolts to the foundation, access door to the internal junction box
( Conical upper column length 2450, decorated base with leaves, longitudinal grooves, upper capital, end prepared for lighting fixture or bracket connection.
( Junction box 235x70x45, class II double insulated, CEI EN 60668-1, CEI EN 60998-2-1, box IP54, 4 poles 3 ways, rear in/out 4x2.5-16 sqmm, looping 4x1,5-4 sqmm, 1 sectionable fuseholder 8,5x31,5 max 10A on DIN rail. 

Cast iron item are metalized to be protected against corrosion. 

External painting, if any, with colour from our colour card; black, anthracite, brown, shadow, granite graphite, green, reseda, steel oversee,  powder, aluminum,  ruby, chestnut, ivory, white) rough effect, obtained with thermosetting powders cycle including: cleaning from zinc coating burs; smoothing of the surfaces by means of a light mechanic device; cleaning of the surfaces in order to eliminate grease or dirty and create a good adherence base; application by means of electrostatic spray of polyester powder suitable for galvanized surfaces for outside installation, in order to reach  60/80 micron thickness; polymerization into oven at constant temperature of approx. 200° for 40-50 minutes, package for each column, by banding with tissue 100% polyester, (no pluriball), in order to avoid damages during the handling phase. The characteristics of the obtained coat will be: average thickness 60 micron, resistance to checkering test  ISO2409, resistance to crash test to UNI8901
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